## Slide 1
Chu, P.H., Kleinhenz, N., Persson, N. et al., Chem. Mater., 2016, 28, 9099–9109
Persson, N. E. et al. ACS Appl. Mater. Interfaces 2017, 9, 36090–36102.
Backbone transport
UV Irradiation
Aging
+
Transport through π-π stacks
µ = 0.2
µ = 0.12
Blade Coated
+
Nanofiber Preparation
Imaging this interface
(P3HT/SiO2)
Alignment & Mobility Anisotropy
1 µm
gtfiber.github.io
* Polymer backbone perpendicular to fiber backbone

## Slide 2
Charge
Transport
2 µm
0.05 mm/s
5 mm/s
Coat
gtfiber.github.io
Persson, N. E. et al. ACS Appl. Mater. Interfaces 2017, 9, 36090–36102.
Alignment & Mobility Anisotropy
P(NDI2OD-T2) – n-type semiconducting polymer – polymer backbone || fiber backbone

## Slide 3
Data Structures
Same resolution
Pixel is white (1) if it’s a fibrillar (crystalline) region
Data: <image name>_bw_array.txt
Data: <image name>_acm_array.txt
Same resolution
Every pixel has an orientation between
[-90, +90), in degrees off of the horizontal
But, in the image above, the color is only plotted for fibrillar pixels (for clarity)
There is no directionality to the orientation: θ = θ + 180
P3HT: chain backbone perpendicular to fibril orientation
N2200: chain backbone parallel to fibril
Original Image
512 x 512 (original AFM resolution)
Grayscale
P3HT: 5 um image (10 x 10 nm pixels)
N2200: 10 um image (20 x 20 nm pixels)